reuse of waste containing biAXIALLY oriented polypropylene in the manufacture of WOOD-PARTICLE BOARDS

REAPROVEITAMENTO de RESÍDUOS CONTENDO POLIPROPILENO BIORIENTADO na fabricação de PAINÉIS DE MADEIRA aglomeradA

RESUMO

O objetivo principal deste trabalho foi a incorporação de diferentes porcentagens de resíduos provenientes da fabricação de rótulos e etiqueta, mais conhecidos como aparas, contendo polipropileno biorientado (BOPP) em painéis de madeira aglomerada, visando seu reaproveitamento. Foram realizados testes físicos, químicos e mecânicos. De acordo com os resultados obtidos pôde-se observar a importância de uma mistura homogênea dos materiais,  e o controle do pH. A incorporação de resíduos contendo BOPP em painéis de madeira aglomerada pode ser uma alternativa promissora de disposição final para este resíduo, pois desenvolve um subproduto e incentiva o desenvolvimento sustentável.

PALAVRAS - CHAVE: Incorporação; aparas; aglomerado.

ABSTRACT

This study analyzed the incorporation of different percentage of waste from the manufacture of labels, commonly known as chips, containing biaxially oriented polypropylene (BOPP) into wood particle boards, aiming its reuse. Physical, chemical and mechanical tests were performed. The results indicated the importance of a homogeneous mixture of materials, and pH control. The incorporation of waste containing BOPP in wood particle boards may be a promising alternative for disposal of this waste, given the development of a by-product, thus encouraging sustainable development.

KEYWORDS: Incorporation; paper scrap; particle board.

INTRODUCTION

Solid waste has caused increasing concern worldwide because of the large amount generated and also the difficulty of environmentally safe disposal. This can cause serious environmental problems when disposed in inappropriate places like landfills or dumps, causing soil degradation, contamination of groundwater and water sources and air pollution. (Vitorino, Monteiro & Vieira, 2009; Wolff, Schwabe & Conceição, 2014).

There are numerous forms of waste reuse in civil and architectural construction, for example: manufacture of ceramic bricks incorporating industrial laundry sludge (Herek, Junior & Pavezzi, 2009), production of tiles with the addition of industrial waste and fiber (Soares, Leal & Costa, 2010), manufacture of alternative boards incorporating rice husk into wood particle boards using tannin-formaldehyde based resin (Sales, Souza & Almeida, 2011), incorporation of different percentages of bamboo into boards made of wood of pine and eucalyptus (Vivian et al., 2012), among others.

The demand for environmentally friendly materials for construction and architectural manufacturing has led to the development of compounds using natural fibers, especially lignocellulosic materials such as wood, which has been used as a reinforcing agent in polymer matrices for the production of particle boards and composites since the production of synthetic fibers shows a high environmental cost (Barros Filho, Mendes & Novack, 2011).

According to the Brazilian technical standard 10.004 (ABNT, 2004), wood waste can be classified as class II waste, because it is a natural and biodegradable waste. An alternative to obtain a higher value-added product is the use of these residues from the timber industry (in the form of costaneiras, refilos and shavings) for the production of particle boards (Iwakiri, Caprara & Saks, 2005).

The binder for the production of particle boards can be a urea-formaldehyde (UF) type resin, which is widely used in the manufacture of particle boards forming a composite material, besides being a stabilizer economically viable found in the market (Silva, Penna & Logsdon, 2008).

A composite consists of reinforcement (structural component) and a matrix (matrix component), which is continuous and surrounds the other phase. These components do not dissolve up or completely mischaracterize, moreover, act synergistically, and properties of the set are superior to those of each individual component.

Plastic materials based on synthetic products are increasingly used in our daily lives, mainly due to their low cost, easy processing, high applicability and durability. The latter characteristic is the greatest disadvantage of their application in the manufacture of disposable packaging.

A biaxially oriented polypropylene pre-polymer used in the manufacture of labels and stickers may be used as a crosslinking agent for obtaining wood particle boards. The main advantages of polypropylene for the manufacture of flexible packaging, at the expense of other materials, include: low cost, high solvent resistance, easy molding and coloration and high resistance to bending fracture, high impact resistance and good thermal stability.

Industries manufacturing labels and stickers, aiming to provide information to consumers, require materials with high print quality, by using this biaxially oriented polypropylene film, as they meet the desired goal with the use of this material.

In the process of manufacturing these labels and stickers, many paper scrap are left over. These chips are adhesive, so, they have glue in their composition. They are generated by companies in large quantities and do not have any recycling or reuse, then being directed for waste collecting companies, and these direct them to industrial landfill.

Wood particle boards containing fiber are characterized by transformation of wood into small particles, dried, mixed with thermosetting synthetic resin, randomly distributed, shaped under heat and pressure generating a board. This process, when using waste from different sources, can contribute to promoting the proper disposal of waste (Chamma & Leão, 2008).

Factors that influence the production of wood particle boards as final product are: specific mass, density, particle geometry, moisture content, type and amount of resin, mattress forming method and pressing parameters (Weber & Iwakiri, 2015).

Considering the above, this study presents a sustainable alternative to the use of waste from the manufacture of labels and stickers containing biaxially oriented polypropylene. In this way, we sought to make them primarily useful by replacing wooden parts with a percentage of this waste, obtaining a quality product for commercial use in the furniture industry.

MATERIAL AND METHODS

Collection and preparation of materials

The wood used in this work came from Pinus hardwood logging, in the form of sawdust, of the Lopes and Diniz carpentry, city of Londrina, state of Paraná.

There were collected 25 kg of chips (waste of labels and stickers) containing biaxially oriented polypropylene (waste) and polyurethane based glue, of the Inovaflex Rótulos and Etiquetas, city of Maringá, state of Paraná.

Waste containing biaxially oriented polypropylene were purchased for this work in the form of roll paper, weighing 2-5 kg each roll with width ranging between 10 and 15 cm. After manual cutting of this material, it was obtained samples in mesh particle size of 1.2 mm, 0.6 mm, 0.4 mm, 0.25 mm, 0.15 mm and 0.075 mm, according to NBR 7181 (ABNT, 1984). The materials, wood and waste were stored individually in plastic bags with a capacity of 50 kg.

It was also purchased 6 kg of urea formaldehyde resin (UF) and 500 g of catalyst ((NH4)2(SO3)) PA of Vetec.

Wood and waste were analyzed for the following parameters: moisture and density and pH, according to the methodology of the Adolfo Lutz Institute (Instituto Adolfo Lutz, 1985); particle size, NBR 7181 (ABNT, 1984), and metals NBR 10.004 (ABNT, 2004).

The opening of the samples was held by digestion with aqua regia. These solutions were subjected to reading of metals by plasma atomic absorption spectrophotometer, model ICP - OES - Optima - 5200/Plasma - Perkin Elmer. Solubilization and leaching tests were performed according to NBR 10.005 and NBR 10.006 methodologies, both of ABNT (2004), respectively.

Production of wood particle boards

The manufacture of wood particle boards was performed at the Madeireira Ibiporã, Ibiporã, state of Paraná. At this stage, it used a hydraulic press with heating, SIRMA, according to (Chama & Leão, 2008); (Battistelle, Santos, & Miyazato, 2006); (Li,  Cai & Winandy, 2010).

The density of the boards was set to 700 kg.m-3 to obtain medium density boards.

After weighing and mixing the materials, the mass of particles was shaped and compressed forming a particle mattress. This process was conducted in a shape with 1000x400x100 mm dimensions. This particle mattress wrapped in aluminum foil was cold pre-pressed and then hot pressed.

After reaching thermal equilibrium, samples of each board was taken and identified as for quantity and size. Specimens were identified for physical and mechanical tests, according to NBR 14.810-3 (ABNT, 2006). Chemical analyses were performed according to NBR 10.004 (ABNT, 2004).

Characterization of wood particle boards

Boards were characterized by tests of density, moisture content, water absorption, thickness swelling and static bending according to NBR 14.810-3 (ABNT, 2006); which was performed in a universal testing machine (EMIC) with 5 KN load cell.

Statistical analysis

This was a complete 23 factorial design with central point, assessing the factors: amount of resin, waste and temperature at two levels. Statistical data were analyzed using the software Design-Expert®. Table 1 shows the levels and factors used to perform the experimental design.

Table 2 lists the lower (-1) (lower values) and higher (+1) levels (higher values) and central points (0) of the variables amount of resin (A), amount of waste (B) and temperature (C). All experiments were performed in duplicate and at random, which generated a total of 20 experiments.

Table 1 – Factors and levels of factors used in the complete 23 factorial design for the production of wood particle boards.

| Factor | Variable | Unit | Type | Level (-1) | Level (0) | Level (+1) |
| --- | --- | --- | --- | --- | --- | --- |
| A | Resin | % | Numerical | 6 | 12 | 18 |
| B | Waste | % | Numerical | 10 | 30 | 50 |
| C | Temperature | ºC | Numerical | 130 | 150 | 170 |

Table 2- Complete 23 factorial design, in duplicate, with central point.

| Samples | Factors |  |  |
| --- | --- | --- | --- |
|  | A Resin/% | B Waste/% | C Temperature/ºC |
| 1.1 and 1.2 | (-1) 6 | (-1) 10 | (-1) 130 |
| 2.1 and 2.2 | (-1) 10 | (+1) 50 | (-1) 130 |
| 3.1 and 3.2 | (+1) 18 | (-1) 10 | (-1) 130 |
| 4.1 and 4.2 | (+1) 18 | (+1) 50 | (-1) 130 |
| 5.1 and 5.2 | (-1) 6 | (-1) 10 | (+1) 170 |
| 6.1 and 6.2 | (-1) 6 | (+1) 50 | (+1) 170 |
| 7.1 and 7.2 | (+1) 18 | (-1) 10 | (+1) 170 |
| 8.1 and 8.2 | (+1) 18 | (+1) 50 | (+1) 170 |
| 9.1 and 9.2 | (0) 12 | (0) 30 | (0) 150 |
| 10.1 and 10.2 | (0) 12 | (0) 30 | (0) 150 |

RESULTS AND DISCUSSION

Material characterization

Table 3 presents the results of the physical tests on wood particles and waste. The manufacture of wood particle boards requires that the particles have moisture about 3-12%, allowing greater penetration of glue, because too dry particles make handling difficult, requiring a greater amount of resin, and producing boards of ease of disintegration, and very moist particles can interfere with the quality of the panel in the pressing process, like the formation of bubbles and bursting of the boards (Iwakiri et al., 2005). The moisture content found in the raw materials is within the optimum range for producting the panels, thus favoring the use of these materials.

The density of the waste particles was higher than that of wood particles, which may result in low values of mechanical properties, given the presence of more voids in the material, favoring the formation of bubbles during the heating process for the manufacture of wood particle boards.

In relation to the pH, the value found for waste was 6.8 and for wood particles was 4.2. The pH influences the final quality of the manufactured board. Cure rates of formaldehyde-based resin are dependent on the pH (Nemli, Gezer & Yildiz, 2006); low pH may cause the pre-cure of the resin. When there is a pre-curing of a resin, board layers are weak, as the resin cures before the compression of the particles and therefore, when the press closes, the resin bonds are broken. This may also have contributed to the low values of mechanical properties.

Table 3- Physical properties of particles of wood and waste.

| ANALYSIS | RESULTS |  |  |
| --- | --- | --- | --- |
|  | Wood | Waste | Standard |
| Moisture (%) | 8.0 | 3.60 | 3.00 a 12.00 |
| Density (g/mm) | 1.53 | 5.06 | - |
| pH (mm) | 4.2 | 6.8 | - |

Figure 1(a) shows the particle size curve for the waste. The diameter of waste particles is within the range 0.08-2.0 mm, and most was retained on 16 mesh sieve, i.e., 1.2 mm.

The particles resulting from waste cutting are large, which may affect the board resistance, because smaller particles increase the contact surface, enhancing the absorption of the resin for generating a resilient board. Larger particles can adversely affect the quality of the final product due to internal flaws in the particles, namely, a larger number of voids in the material (Vignote & Jimécez, 1996).

Considering the studies on particle diameters mentioned above and the incorporation capacity of the waste, values of the average geometric diameter (AGD) of samples were reduced to the maximum, and used in particulate form, which distribute better the stresses of the material and produce fewer voids inside the plates, resulting in a stronger product (Cabral, Schalch & Dal Molin, 2007).

Figure 1(b) illustrates the particle size curve for the wood. The highest percentage of particles (45.56%) corresponds to the fraction of particles retained on the mesh (≤ 4.0 mm). The mesh (1.40 ≤ x ≤ 2.0 mm) corresponds to 36.85% of the material composition, while the content retained on the meshes (1.0 ≤ x ≤ 0.50 mm) is around 14.76%. Wood fractions used were those retained on the mesh 1.40 mm, in order to improve the homogenization of the mass and absorption of the resin, with the increase of the contact surface.

Emphasized that fine particles are an interesting option, since his study on the pressing cycle indicated that there was no need to increase the resin content (Albuquerque, 2000). This same author reported that such particles behave in a more stable and homogeneous way that coarse particle boards.

In the reported tests, it was observed that the use of small particles favors the perpendicular tensile strength but causes a reduction in the rupture stress and the elasticity modulus (Cabral et al., 2007). As a result, it was used DGM particles of the intermediate mesh to benefit both the mechanical properties.

percentagem (%)

percentagem (%)

particle diameter (mm)

particle diameter (mm)

(a)

(b)

Figure 1 – Particle size curve for particles of (a) waste and (b) wood. Test performed according to NBR .

Table 4 presents the metals and their respective values determined in the waste sample, and the results for the solubilization and leaching tests.

The metals found in the waste were aluminum, copper, chromium, iron and nickel. These metals are derived from dyes present in the material.

All values of the metals analyzed (Table 4) are within the range set by the NBR 10004 (ABNT, 2004), leaching tests (NBR 10005) and solubilization test (NBR 10006). Only the metals lead and chromium have normative standards, but they were no longer detected in the solubilization test.

The analysis of metals in wood, leached and solubilized extracts did not detect the presence of any of the metals listed in Table 4, metals required for analysis by NBR 10004 (ABNT, 2004). Thus, materials, waste and wood, are in accordance with the technical standard NBR 10004 (ABNT, 2004), not exceeding the maximum limits, indicating that these samples present no hazard characteristics and are then classified as Class II waste, non-hazardous and inert.

Table 4 – Metal levels determined in the sample of waste, using the atomic absorption, leaching and solubilization method

| Waste |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| METALS | RESULTS (mg/kg) |  |  |  |  |
|  | Metals | Leaching | Leaching limit NBR 10004 | Solubilization | Solubilized limit NBR 10004 |
| Aluminum | 1.6 | 1.0 | - | n.d* | 2.00x10-1 |
| Arsenic | n.d* | n.d* | 1.0 | n.d* | 1.0x10-2 |
| Barium | n.d* | n.d* | 7.00x101 | n.d* | 7.00x10-1 |
| Cadmium | n.d* | n.d* | 5.00x10-1 | n.d* | 5.00x10-3 |
| Calcium | n.d* | n.d* | - | n.d* | - |
| Lead | 1.4 | 2.10x10-1 | 1.00 | n.d* | 1.00x10-3 |
| Copper | 0.20x10-1 | n.d* | - | n.d* | 2.00 |
| Chromium | 1.0x101 | 1.20x10-1 | 5.00 | n.d* | 5.00x10-2 |
| Iron | 5.2x102 | 1.3x10-2 | - | n.d* | 3.00x10-1 |
| Nickel | 3.5x101 | n.d* | - | n.d* | - |
| Manganese | n.d* | n.d* | - | n.d* | 1.0x10-1 |
| Mercury | n.d* | n.d* | 1.0x10-1 | n.d* | 1.0x10-3 |
| Potassium | n.d* | n.d* | - | n.d* | - |
| Silver | n.d* | n.d* | 5.0 | n.d*1 | 5.0x10-2 |
| Selenium | n.d* | n.d* | 1.0 | n.d* | 1.0x10-2 |
| Sodium | n.d* | n.d* | - | n.d* | 2.00x102 |
| Zinc | n.d* | n.d* | - | n.d* | 5.00 |
| n.d* - undetected |  |  |  |  |  |

Analyses on wood particle boards

The results obtained in the tests of density, moisture content, thickness swelling, water absorption and modulus of elasticity (MOE) are shown in Table 5. Density values were below the value set by the ABNT NBR 14.810-2 (2006) to classify a wood particle board as having medium density (between 551 kg.m-3 and 750 kg.m-3).

This is due to two main factors, one is the failure in mixing, since the process was carried out manually; and the other is the concentration of UF resin used, as this characteristic was also found in the literature (Silva et al., 2008), in which the homogeneous distribution of the resin is critical to provide uniformity throughout the product.

Table 5 – Mean values of the physical tests of density, moisture, thickness swelling and water absorption and static bending (MOE) in wood particle boards.

|  | PARAMETER |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| TREAT. | DENSITY (kg.m-3) | MOISTURE (%) | % IE 2h | % IE 24h | % AA 2h | % AA 24h | MOE (MPa) |
| 1.1 and 1.2 | 447.59 | 14.23 | 9.37 | 16.40 | 65.56 | 110.53 | 5.61 |
| 2.1 and 2.2 | 391.92 | 14.27 | 8.20 | 15.05 | 61.72 | 105.17 | 3.17 |
| 3.1 and 3.2 | 410.91 | 15.78 | 7.54 | 12.53 | 66.71 | 89.00 | 3.87 |
| 4.1 and 4.2 | 560.26 | 11.11 | 11.12 | 17.49 | 70.25 | 90.58 | 2.71 |
| 5.1 and 5.2 | 376.10 | 14.62 | 10.47 | 15.92 | 79.58 | 91.19 | 2.82 |
| 6.1 and 6.2 | 310.52 | 19.59 | 4.84 | 8.03 | 67.99 | 84.4 | 2.43 |
| 7.1 and 7.2 | 446.91 | 13.68 | 6.16 | 12.54 | 55.42 | 76.48 | 6.06 |
| 8.1 and 8.2 | 446.23 | 12.99 | 10.77 | 14.52 | 63.82 | 87.05 | 1.96 |
| 9.1 and 9.2 | 514.32 | 12.22 | 5.59 | 13.04 | 49.47 | 70.13 | 3.67 |
| 10.1 and 10.2 | 552.52 | 12.18 | 7.40 | 10.63 | 81.14 | 91.82 | 2.47 |

With the aid of data in Table 5 and the software Design Expert, we obtained the results of the planning for the responses of the moisture content and the modulus of elasticity (MOE). These results of planning, considering the ANOVA, are listed in Tables 6 and 7, respectively. Regarding the MOE, NBR 14.810-2 (ABNT, 2006) does not set a threshold value.

The P value (Prob> F) denotes the probability of obtaining a test statistic equal to or more extreme than that observed in a sample under the null hypothesis. In other words, assuming the P-value of 0.0500, it can be concluded that there is a chance that only 5.00% the result is a coincidence. Therefore, P values below 0.0500 represent greater reliability to the test (Bussab & Morettin, 2003).

Thus, in Table 6, the moisture content for the adopted model was significant because the P-value obtained was 0.0223, and the lack of fit was 0.1935, greater than 0.05, which makes this lack of fit non-significant, which is desirable.

Among the major effects, only the amount of resin was significant. The effects of AC and BC interactions were statistically significant for the model, with P <0.05, as the sum of the squares indicates that the temperature influences the model, being statistically influential on responses of AC and BC interactions.

The F-value represents the difference between the factor and the sample. This value is calculated by dividing the variance between the factorial by the variance of each sample. The higher the F-value, the greater the difference between groups compared to the difference between each experiment. From Table 6, it is observed that the amount of resin was the most influential factor in the manufacture of particle boards. This can also be observed by analyzing Figure 3(a), where it is shown the response surface for the moisture content depending on the amount of waste and resin. Thus, the increase in the amount of resin reduces the moisture content, which positively influences the manufacture of wooden boards. Data on Figure 3(a) indicate that the factors influencing positively the manufacture of particle boards were the amount of resin and the temperature.

Summary of ANOVA (Table 7) run for the modulus of elasticity (MOE) evidenced that the model was significant with P equal to 0.0002, and the lack of fit was 0.1020, namely non-significant, proving that the manufactured board has satisfactory conditions for this parameter.

As observed in the moisture analysis, the amount of resin was again the factor with greater influence on the model and the interaction between the resin amount and the temperature was also significant, since the resin improves the structural strength of the particle board. Figure 3(b) may confirm this, where the response surface obtained for MOE analysis according to the amounts of resin and waste show that increasing the amount of resin significantly improves the load supported by wooden boards.

Table 6 – Analysis of variance (ANOVA) for factors A, B and C and their interactions on the response of moisture content.

| SOURCE | SQUARED SUM | DEGREES OF FREEDOM | SQUARED MEAN | F-TEST | P |
| --- | --- | --- | --- | --- | --- |
| MODEL | 133.44 | 7 | 19.6 | 3.73 | 0.0223 |
| A – resin | 39.06 | 1 | 39.06 | 7.64 | 0.0172 |
| B – waste | 5.06 | 1 | 5.06 | 0.99 | 0.3394 |
| C - temperature | 0.062 | 1 | 0.062 | 0.012 | 0.9138 |
| AB | 7.56 | 1 | 7.56 | 1.48 | 0.2473 |
| AC | 33.06 | 1 | 33.06 | 6.47 | 0.0258 |
| BC | 45.56 | 1 | 45.56 | 8.91 | 0.0114 |
| ABC | 3.06 | 1 | 3.06 | 0.70 | 0.4540 |
| Residual | 61.36 | 12 | 5.11 | - | - |
| Lack of fit | 9.11 | 1 | 9.11 | 1.92 | 0.1935 |
| Pure error | 52.25 | 11 | 4.75 | - | - |
| Total | 194.80 | 19 | - | - | - |

Table 7 - Analysis of variance (ANOVA) for factors A, B and C and their interactions on the response of MOE.

| SOURCE | SQUARED SUM | DEGREES OF FREEDOM | SQUARED MEAN | F-TEST | P |
| --- | --- | --- | --- | --- | --- |
| MODEL | 28.44 | 7 | 4.06 | 10.80 | 0.0002 |
| A - resin | 0.062 | 1 | 0.062 | 0.17 | 0.6907 |
| B - waste | 14.06 | 1 | 14.06 | 37.40 | <0.0001 |
| C – temperature | 0.56 | 1 | 0.56 | 1.50 | 0.2448 |
| AB | 0.56 | 1 | 0.56 | 1.50 | 0.2448 |
| AC | 5.06 | 1 | 5.06 | 13.46 | 0.0032 |
| BC | 0.56 | 1 | 0.56 | 1.50 | 0.2448 |
| ABC | 7.56 | 1 | 7.56 | 20.11 | 0.0007 |
| Residual | 4.51 | 12 | 0.38 | - | - |
| Lack of fit | 1.01 | 1 | 1.01 | 3.18 | 0.1020 |
| Pure error | 3.50 | 11 | 0.32 | - | - |
| Total | 32.95 | 19 | - | - | - |

MOE (MPa)

moisture (%)

B - waste (%)

A - resin (%)

B - waste

A - Resin (%)

Figure 3 - (a) Response surface obtained for moisture content according to factors A and B; (b) Response surface obtained for MOE according to factors A and B.

CONCLUSIONS

The production of an alternative product offers economic, social and environmental benefits related to the lower consumption of resources and the reuse of materials. The production of wood particle boards with incorporation of waste containing axially oriented polypropylene is an option that meets these benefits when working at high temperature and low incorporation of waste.

Wood particle boards incorporating waste were not classified as having medium density, as they did not reach values in the range of 551-700 kgf/cm2, and were characterized as low density boards.

All the results were satisfactory. It is necessary a more homogeneous mixture of materials to obtain better results. It was not possible to achieve a homogeneous distribution of the resin, and the pH of wood particles used directly affected the faster curing of the resin. These parameters had high influence on the low density of the board obtained in this work, but adjustments can be taken during the manufacturing process to achieve these parameters.

In accordance with the results, the maintenance of high resin content is necessary to maintain the quality of the obtained boards.

REFERENCES

ABNT NBR 7.181, Solo – Análise Granulométrica – Procedimento, Rio de Janeiro, 1984.

ABNT NBR 10.004 (2004), Resíduos Sólidos: Classificação, Rio de Janeiro.

ABNT NBR 10.005 (2004), Resíduos Sólidos: procedimento para obtenção de extrato lixiviado de resíduos sólidos, Rio de Janeiro.

ABNT NBR 10.006 (2004), Resíduos Sólidos: procedimento para obtenção de extrato solubilizado de resíduos sólidos, Rio de Janeiro.

ABNT NBR 14.810-1 (2006), Chapas de madeira aglomerada. Parte 1: Terminologia, Rio de Janeiro.

ABNT – NBR 14.810-2 (2006), Chapas de madeira aglomerada. Parte 2: Requisitos, Rio de Janeiro.

ABNT – NBR 14.810-3 (2006), Chapas de madeira aglomerada. Parte 3: Métodos de ensaio, Rio de Janeiro.

Albuquerque, C. E. C. (2000). Desenvolvimento de um sistema de pré-secagem de partículas de Pinus e de Eucalipto, para a produção de chapas de madeira aglomerada. 7(1), 104-120.  Rio de Janeiro, RJ: Floresta e Ambiente, Seropédica.

Barros Filho, R. M., Mendes, L. M.. Novack, K. M., Aprelini, L. O., & Botaro, V. R. (2011). Hybrid chipboard panels based on sugarcane bagasse, urea formaldehyde and melamine formaldehyde resin. Industrial Crops and Products (Print),33, (369-373).

Battistelle, R.A.G., Santos, M.F.N., Miyazato, T., Redivo, C., & Freitas, P.N.P (2006). Estudo comparativo entre chapas de partículas confeccionadas com diferentes resíduos e sua aplicação em design de produtos. In: XIII SIMPEP Bauru, SP.

Bussab, W. O., & Morettin, P A. (2003). Estatística básica. 5ª. Ed. São Paulo, SP: Saraiva.

Cabral, A. E. B. , Schalch, V. , Dal Molin, D. C. C., Ribeiro, J. L. D.(2007) . Modelagem da resistência à compressão de concretos produzidos com agregados reciclados de RCD. Revista Minerva, (4), 75-84.

Chamma, P. V. C.,  & Leão, A. L. (2008). Aproveitamento de resíduos sólidos na produção de painéis para aplicações arquitetônicas. Revista Energia na Agricultura, ,3 (2), 73-87.

Colli, A., Vital, E. R., Carneiro, A. C. O., Silva, J. C., Carvalho, A. M. M. L., & Della Lucia, R. M. (2010). Propriedades de chapas fabricadas com partículas de madeira de paricá (Schyzolobium amazonicum Huber ex. Ducke) e fibras de coco (Cocos nucifera L.). Revista Árvore, Viçosa, MG, 34 (2), 333-338.

Herek, L. C. S., Júnior, A. T. S., Pavezzi, C. C. Pavezzi, Bergamasco, R., & Tavares, C. R. G. (2009). Incorporação de lodo de lavanderia industrial na fabricação de tijolos cerâmicos. Revista Cerâmica, 55 (335), 389-392.

Instituto Adolfo Lutz (1985). Normas Analíticas do Instituto Adolfo Lutz: Métodos químicos e físicos para análise de alimentos. 3º Ed., (334). São Paulo, SP: IMESP.

Iwakiri, S., Caprara, A. C., Saks, C. D. O., Guisantes, S. P., Franzoni, J. A., Krambeck, L. B. P., & Rigatto, P. A. (2005). Produção de painéis de madeira aglomerada de alta densificação com diferentes tipos de resinas. Scientia Forestalis, 68 ,(39-43).

Li, X.,  Cai, Z., Winandy, J. E., & Basta, A. H. (2010). Selected properties of particleboard panels manufactured from rice straws of different geometries. Bioresource Technology, 101, ( 4662–4666).

Nemli, G., Gezer, E.D., Yildiz, S., Temiz, A. & Aydin, A. (2006). Evaluation of the mechanical, physical properties and decay resistence of particleboard made from particules impregnated with Pinus butia bark extractives. Biores Technol., (97), 2059-2064.

Pizzi, A. (1994). Advanced wood adhesives technology. 370, New York, EUA: Marcel Dekker.

Sales, A., de Souza, F. R., & Almeida, F. C. R (2011). Mechanical properties of concrete produced with a composite of water treatment sludge and sawdust. Construction & Building Materials, 25, (2793-2798).

SENAI - RS/UNIDO/UNEP  (2003). Centro Nacional de Tecnologias Limpas. Implementação de Programas de Produção Mais Limpas. 41 p. Porto Alegre, RG. Disponível em: < http://wwwapp.sistemafiergs.org.br>. Acesso em: 19 fev. 2012.

Silva, A. M.,  Penna, J. E., Logsdon, N. B., & Abreu, J. G.(2008). Estudo da Variação Radial das Densidades Aparente e Básica da Madeira de Vochysia Guianensis Aubl. (Cambará ou Quaruba-branca ) Vochysiaceae no Sentido Medula/Casca ao Longo de uma Seção Diametral do Tronco. In: XI Encontro Brasileiro em Madeiras e Estruturas de Madeira, Londrina, PR. XI Encontro Brasileiro em Madeiras e Estruturas de Madeira. Londrina, PR.: UEL.

Soares, E. A., Leal, A. F., & Costa, F. N. M. (2010). Produção de telhas com resíduos industriais e fibras. Revista Educação Agrícola Superior, 25 (2), 87-92.

Vignote, P. S., Jimécez, P. F. J. (1996).  Tecnología de la madera. Madrid, Spain: Ministerio de Agricultura, Pesca y Alimentación.

Cabral, C. P., Vital, B. R., Della Lucia, R. M., & Pimenta, A. S. (2007). Propriedades de chapas de aglomerado confeccionadas com misturas de partículas de Eucalyptus spp e Pinus elliottii. Revista Árvore, 31(5), 88-96.

Vitorino, J. P. D., Monteiro, Vieira, S. N.,& Vieira, C. M. F.  (2009). Caracterização e incorporação de resíduos provenientes de Estação de Tratamento de Água em cerâmica argilosa. Cerâmica, 55, (385-392).

Vivian, M. A., Santini, E. J., Modes, K. S., Santini, E. J., Carvalho, D. E., Morais, W. W. C.,... Gatto, D. A.(2012). Estimativa dos Módulos de Elasticidade e Ruptura da Madeira de Eucalyptus cloeziana F. Muell por Meio de Método Não Destrutivo.  Ciência da Madeira,  3, (91-101).

Weber, C., & Iwakiri, S. (2015). Utilização de Resíduos de Compensados, MDF e MDP para Produção de Painéis Aglomerados. Ciência Florestal (UFSM. Impresso), 25 (405-413).

Wolff, E., Schwabe, W. K., & Conceição, S. V. (2015). Utilization of water treatment plant sludge in structural ceramics. Journal of Cleaner Production, 96, (282-289).